

Professional Cubicle Curtains

1-800-258-8817 • [custsvc@ModoMed.com](mailto:custsvc@modomed.com)

[www.ModoMed.com](http://www.modomed.com/)

**CUBICLE CURTAIN CARE AND SPECIFICATIONS**

**FABRIC:** Allegro

**FEATURES:**

* Fabric is treated with Zinc Pyrithione (ZnP) - a durable, effective and safe antimicrobial compound.
* Zinc Pyrithione (ZnP) stops growth of bacteria or fungi upon curtain contact.
* Antimicrobial performance is verified up to 25 washings.
* Zone of inhibition prevents cross contamination and microorganisms from growing on or around fabric.
* Permanently flame retardant passing the NFPA 701 and MVSS-302 vertical flammability test.

**SPECIFICATIONS:**

* Color Type: Dye
* Fabric Content: 100% Polyester
* Weave: Dobby
* Finish: Anti-Microbial Fire-Retardant
* Horizontal Repeat: 0.69”
* Vertical Repeat: 1.38”
* Weight: 5.61 oz./sq. yard

**CARE INSTRUCTIONS:**

*THIS FABRIC CAN BE WASHED OR DRY CLEANED*

*WASH CYCLE:*

Machine wash in water temperature not exceeding 160oF. Using SYNTHETIC detergent.

* DO NOT BLEACH.
* DO NOT EXTRACT.
* AVOID FABRIC SOFTNERS OR OTHER CHEMICAL THAT CONTAINS SILICONE, WHICH AFFECTS FLAMMABILITY.

*DRYING CYCLE:*

* Tumble dry 3-5 minutes on SYNTHETIC cycle (110oF.) until damp dry, and remove immediately.

*FINISHING:*

* No finishing if fabric is re-hung at termination of drying cycle. Occasional light touch-up with hand iron (275oF. Maximum) may be desired.
* DO NOT MANGLE.